LIGNOCELLULOUS RAW MATERIALS AND ITS WASTES TRANSFORMATION INTO VALUE-ADDED PRODUCTS

Bohdan Korinenko1, Tetiana Tkachenko1, Oleksandr Pavliuk1, Dmytro Kamenskyh1,2, Vitalii Yevdokymenko1

1. Department of Organic and Petrochemical Synthesis, V.P. Kukhar Institute of Bioorganic Chemistry and Petrochemistry of the NAS of Ukraine, 02094, UKRAINE, Kyiv, 1, Academician Kukhar Str, E-mail: ttv13ttv@gmail.com, kam04@ukr.net, vay.77@ukr.net

2. V. Bakul Institute for Superhard Materials of the NAS of Ukraine, 04074, UKRAINE, Kyiv, 2, Avtozavids’ka Str.

Abstract  The aim of our work was to investigate the possibility of obtaining marketable products (fibrous and microcrystalline cellulose, cellulose acetate, lignosulfonates, oxyaldehydes, fertilizers and primings, etc.) from renewable lignocellulosic raw materials.

Кеуwords  lignocellulosic raw materials, fibrous cellulose, microcrystalline cellulose, cellulose acetate, lignosulfonates, organo-mineral fertilizers, silica.

Introduction

Historically, biomass has been widely used primarily as an energy source. It is also a valuable chemical raw material for the production of almost all petrochemical synthesis products. To date, 20 basic compounds have been identified, which are sufficient for the manufacture of almost the entire range of chemical industry products and which can be obtained from plant biomass [1,2]. Ultimately, the current state of fossil fuels has emphasized the future development of the chemical industry market, which is predominantly focused on plant biomass. The attention paid in recent decades to renewables is reflected in many scientific reports [3-11].

Therefore, considering that Ukraine is an agrarian country, it is expedient to find ways to obtain marketable products from lignocellulosic raw materials and its waste.

Materials and methods

The lignocellulosic raw materials selected were its waste, as well as industrial crops, namely tree crowns (poplar, oak, birch, linden, chestnut, maple), green waste from mowing lawn grass and forbs, fallen leaves (poplar, oak, birch, linden, chestnut, maple), agricultural waste (wheat, barley, rye, oat, rapeseed, soybean straw, corn and sunflower stalks, rice husks, corn cobs) and industrial crops (giant miscanthus, sugar and Chinese miscanthus, sugar sorghum, switchgrass, flax and hemp). The contents of cellulose, hemicellulose, lignin and other chemical components in lignocellulosic raw materials were determined by standard chemical analysis, described earlier [12,13]. All chemical analysis was carried out twice allowing calculating the mean values and standard deviations, which do not exceed 5 %. The inorganic components were determined using Expert 3L XRF (INAM, Ukraine). The phase identification of the products was examined under X-ray diffraction (XRD) using the MiniFlex 300/600 diffractometer (Rigaku, Japan). The diffraction patterns were recorded using Cu-Kα radiation (λ = 0.15418 nm), the operating voltage of 40 kV and a current of 15 mA. XRD pattern of samples was obtained in the 2θ range between 2o and 80o with a step of 0.02o. FTIR analysis of the obtained products was performed using IRAffinity-1S FTIR spectrometer (Shimadzu, Japan) equipped with a Quest ATR Diamond GS-10800X (Specac, UK) within the wavenumber range of 4000 to 400 cm-1. The porous properties of the products were studied using N2 adsorption at −195.8 °C on the specific surface area and porosity analyser Nova 1200e (Quantachrome, USA). Prior to analysis, 0.23-0.24 g of sample was degassed at 120 °C for 3 h to remove previously adsorbed gases and dead space by vacuum pump to cool down the sample at room temperature. NovaWin 11.04 software was used to calculate the parameters of the porous structure, namely, the specific surface area of SBET (multipoint BET method in the range of p/p0 0.03–0.65); the specific surface area without taking into account micropores St and the volume of micropores Vtmicro - by the t-method (Vα-Smicro - alpha-S method), as well as the specific surface area of micropores - by the formula Stmicro = SBET - St; some of these parameters were also calculated by the DFT method, as was the pore size distribution using selected models. The surface morphology was investigated with atomic force microscope (AFM) NT-206 (Company with double liability “Microtestmachines”, Belarus) equipped with standard sonde CSC37 and rigidity of console 0.3-0.6 N/m. The scan was run in a contact static mode at 10 mcm/s with a step of 0.3 nm. Samples (4 mg) after grinding for 10 min (only for powders) stirred in ethyl alcohol (5 ml) for 15 min. The resulting suspension (0.25 ml) was applied to quartz glass and dried at 50 oC to a constant weight. Then the scan was performed on AFM. The scanning electron microscopy (SEM) images were taken using Zeiss Evo-10 (Carl Zeiss Microscopy, USA) microscope working at 20.0 kV. Thermogravimetric analysis (TGA) and differential scanning calorimetric analysis (DSC) were performed with a PT1600 TG-DTA/DSC (STA Simultaneous Thermal Analysis, LINSEIS Messgeräte GmbH, Germany). The samples (13.0 ± 0.1 mg) were collected in a standard corundum pan. The scan was run at 5 °C/min under a flow of air. The mass change was measured from 15.8 to 100 °C. The sample was analysed three times.

Results

Chemical analysis of tree crowning waste (poplar, oak, birch, linden, chestnut, maple), green waste from mowing lawn grass and forbs, fallen leaves (poplar, oak, birch, linden, chestnut, maple), agricultural waste (wheat, barley, rye, oat, rapeseed, soybean straw, corn and sunflower stalks, rice husks, corn cobs) and industrial crops (giant miscanthus, sugar and Chinese miscanthus, sugar sorghum, switchgrass, flax and hemp) was carried out. The results of the research are presented in Table.

Table 1

Composition of lignocellulosic biomass, % mass in a.d.m.

| Raw material | Ash | Pitches and fats | Water-soluble substances | Cellulose | Hemi- cellulose | Lignin | Other |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Hemp hurd | 2.7 | 0.7 | 3.8 | 48.4 | 25.8 | 20.9 | 0.4 |
| Hemp fiber | 1.5 | 0.8 | 5.3 | 85.3 | 6.3 | 2.1 | 0.2 |
| Flax | 5.4 | 1.9 | 8.75 | 48.0 | 27.1 | 14.06 | 0.19 |
| Switchgrass | 5.4 | 2.0 | 7.7 | 46.7 | 23.0 | 13.8 | 1.4 |
| Wheat straw | 6.5 | 1.2 | 14.5 | 46.5 | 12.9 | 24.6 | 0.3 |
| Rye straw | 6.2 | 1.8 | 7.7 | 46.1 | 15.5 | 28.8 | 0.1 |
| Rape straw | 8.0 | 0.9 | 3.0 | 43.7 | 16.7 | 35.5 | 0.2 |
| Barley straw | 7.6 | 1.2 | 7,2 | 50.0 | 24.2 | 17.1 | 0.3 |
| Oats straw | 7.1 | 2.1 | 16.1 | 40.2 | 10.0 | 31.2 | 0.4 |
| Corn straw | 9.0 | 1.5 | 19.8 | 36,9 | 11.9 | 29.7 | 0.2 |
| Sunflower straw | 14.7 | 2.5 | 16.1 | 27.5 | 10.3 | 43.5 | 0.1 |
| Soybean straw | 4.4 | 0.9 | 4.0 | 46.9 | 11.6 | 36.3 | 0.3 |
| Rice husk | 18.2 | 0.3 | 8.2 | 39.7 | 13.3 | 20.2 | 0.1 |
| Corn cobs | 1.5 | 0.5 | 4.2 | 43.2 | 26.4 | 23.4 | 0.8 |
| Poplar branches | 6.73 | 5.12 | 22.57 | 23.24 | 21.06 | 20.85 | 0.43 |
| Oak branches | 6.94 | 4.00 | 21.07 | 21.71 | 16.35 | 29.41 | 0.52 |
| Birch branches | 5.79 | 8.73 | 18.42 | 16.95 | 27.87 | 21.65 | 0.59 |
| Linden branches | 11.14 | 5.35 | 22.81 | 20.67 | 19.85 | 20.00 | 0.18 |
| Chestnut branches | 9.98 | 3.29 | 17.96 | 18.95 | 25.81 | 24.00 | 0.34 |
| Maple branches | 9.01 | 4.73 | 17.97 | 19.43 | 28.73 | 20.36 | 0.20 |
| Poplar leaves | 14.94 | 5.33 | 11.70 | 25.71 | 16.74 | 25.76 | 0.62 |
| Oak leaves | 8.44 | 9.82 | 17.61 | 16.77 | 21.88 | 25.30 | 1.01 |
| Birch leaves | 31.17 | 14.71 | 8.67 | 21.88 | 15.38 | 12.58 | 0.20 |
| Linden leaves | 18.53 | 5.68 | 4.68 | 25.65 | 24.37 | 21.60 | 0.54 |
| Chestnut leaves | 14.07 | 7.44 | 8.08 | 21.97 | 24.89 | 23.90 | 0.70 |
| Maple leaves | 13.14 | 9.44 | 10.98 | 19.74 | 31.84 | 14.62 | 0.24 |
| Lawn grass | 17.53 | 5.99 | 16.02 | 21.12 | 23.22 | 17.06 | 0.11 |
| Roadside grass | 31.63 | 6.00 | 13.76 | 16.88 | 23.23 | 10.25 | 0.15 |
| Giant miscanthus | 2.80 | 0.29 | 13.01 | 44.71 | 25.31 | 13.77 | 0.12 |
| Sugar sorghum | 8.54 | 0.64 | 30.75 | 31.16 | 19.84 | 9.03 | 0.09 |

It has been established that the waste is characterized by a high content of water-soluble substances and hemicelluloses, which makes them attractive for further processing by bacteria. The works [14,15] show the possibility of obtaining biobutanol from agricultural waste, switchgrass, and green waste from mowing lawn grass and forbs.

Lignocellulosic biomass with high lignin content is a promising raw material for thermolysis to biochar and activated carbon [16-19].

At the same time, technical crops are more attractive for obtaining cellulose, which is currently a pressing issue for our country. Organo-solvent cooking of flax straw, hemp, switchgrass, and soybean straw was carried out [20-23]. The obtained cellulose materials were studied by modern physicochemical methods: low-temperature nitrogen adsorption-desorption, XRD, XRF, FTIR-ATR, AFM, SEM, TGA, and DSC. It was established that the highest yields of fibrous cellulose and MCC ≥90% were achieved when processing technical hemp fibre of the Glesiya variety. Such products were characterized by a low content of inorganic components (0.5 and 0.2%, respectively) and lignin (1.6 and 0.8%, respectively). In terms of their physicochemical characteristics, they are not inferior to world analogues.

From lignin, which was isolated from the cooking liquor to obtain cellulose products or after hydrolysis of the biomass itself, it is possible, in addition to carbon materials, as mentioned above, to obtain sodium and potassium lignosulfonate. The latter was used to obtain fertilizers that have successfully passed field tests [16,24]. Sodium lignosulfonate is widely used as a binder for metallurgy. In addition, lignin is a promising raw material for obtaining oxyaldehydes, as well as high-octane additives to fuels [25-27].

Based on the obtained cellulose products, cellulose acetate was obtained, which in its characteristics is similar to industrial samples, which was confirmed by the FTIR and TGA methods. Thus, the carried out studies showed the possibility of widespread use of lignocellulosic raw materials to obtain a lot of value-added products that are currently imported from abroad.

Conclusions

Thus, we have considered possible directions for the conversion of various lignocellulosic raw materials into marketable products, which can be summarized in Fig. 1.

Fig.1. Scheme of biomass processing directions

Acknowledgments

We thank the Armed Forces of Ukraine for safety to carry out this work. This work was only possible thanks to the resilience and courage of the Ukrainian Army. Our priceless thanks to the heroic soldiers of the Ukraine Army, who protect us from russian aggressor at the cost of their lives.

References

[1]	Aden, A., Bozell, J., Holladay, J., White, J.F., Manheim, A. (2004) Top Value Added Chemicals From Biomass. Vol. 1. Results of Screening for Potential Candidates from Sugars and Synthesis Gas. PNNL NREL. https://www.nrel.gov/docs/fy04osti/35523.pdf

[2]	Kukhar, V.P. (2007) Biomass — potential feedstock for industrial organic synthesis. Catalysis and Petrochemistry. # 15. https://kataliz.org.ua/old/arhiv/15_2007_ua.html

[3]	Chambona, F., Rataboula, F., Pinela, C., Cabiacb, A., Guillonb, E., Essayema, N. (2011) Cellulose hydrothermal conversion promoted by heterogeneous Bronsted and Lewis acids: Remarkable efficiency of solid Lewis acids to produce lactic acid. Applied Catalysis B: Environmental. 105, 171–181. https://doi.org/10.1016/j.apcatb.2011.04.009

[4]	Hao Ma, Bo Shou, Yuqun Li and Dimitris S. (2012) Argyropoulos Conversion of fructose to 5-hydroxymethyl-furfural with a functionalized ionic liguid. BioResourses. 1(7). 533-544. https://api.semanticscholar.org/CorpusID:22427858.

[5]	Avelino Corma, Sara Iborra, and Alexandra Velty (2007) Chemical Routes for the Transformation of Biomass into Chemicals. Chem. Rev. 107. 2411-2502. https://doi.org/10.1021/cr050989d

[6]	Chheda, J.N., Huber, G.W. and Dumesic, J.A. (2007) Liquid-Phase Catalytic Processing of Biomass-Derived Oxygenated Hydrocarbons to Fuels and Chemicals. Angew. Chem. Int. Ed. 46. 7164 – 7183. https://doi.org/10.1002/anie.200604274

[7]	Lichtenthaler, F.W. (1998) Towards improving the utility of ketoses as organic raw materials. Carbohydrate Research. 313. 69-89. https://doi.org/10.1016/S0008-6215(98)00222-5

[8]	Shaw, P.E. (1967) Acid–catalyzed dehydration of D-fructose. Carbohydrate Research. 5. 266-273. https://doi.org/10.1016/S0008-6215(00)80500-5

[9]	Kuster, B.F.M. and Temmink, H.M.G. (1977) The influence of pH and weak-acid anions on the dehydration of D-fructose. Carbohydrate Research. 54. 183-191. https://doi.org/10.1016/S0008-6215(00)84808-9.

[10]	Rosatella, A.A., Simeonov, S.P., Frade, R.F.M. and Afonso, C.A.M. (2011) 5-Hydroxymethylfurfural (HMF) as a building block platform: Biological properties, synthesis and synthetic applications. Green Chem. 13. 754-793. https://doi.org/10.1039/C0GC00401D.

[11] Lanzafame, P., Temi, D.M., Perathoner, S., Spadaro, A.N. and Centi, G. (2012) Direct conversion of cellulose to glucose and valuable intermediates in mild reaction conditions over solid acid catalysts. Catalysis Today. 179. 178-184. https://doi.org/10.1016/j.cattod.2011.07.018.

[12]	Tigunova, O.O., Beiko, N.E., Kamenskyh, D.S., Tkachenko, T.V., Yevdokymenko, V.O., Kashkovskiy, V.I. and Shulga, S.M. (2016) Lignocellulosic biomass after explosive autohydrolysis as substrate for butanol. Biotechnol. Acta. 9(4). 28-34. https://doi.org/10.15407/biotech9.04.028

[13]	Bratishko, V., Tkachenko, T., Shulga, S., Tigunova, O. (2024) Results of chemical studies of parameters and composition of samples of lignocellulose raw materials of communal origin. 23rd International Scientific Conference Engineering for Rural Development. Jelgava, LATVIA. 1008-1015. https://doi.org/10.22616/ERDev.2024.23.TF205

[14]	Tigunova, O.O., Kamenskyh, D.S., Tkachenko, T.V., Yevdokymenko, V.O., Kashkovskiy, V.I., Rakhmetov, D.B., Blume, Y.B. and Shulga, S.M. (2020) Biobutanol production from plant biomass. The Open Agriculture Journal. 14(1). https://doi.org/10.2174/1874331502014010187,

[15]	Bratishko, V., Shulga, S., Tigunova, O., Achkevych, O. (2023) Ultrasonic cavitation of lignocellulosic raw materials as effective method of preparation for butanol production. 22nd International Scientific Conference Engineering for Rural Development Proceedings. 264-268. https://doi.org/10.22616/ERDev.2023.22.TF053

[16]	Tkachenko, T.V., Aksylenko, M.D., Kamenskyh, D.S., Yevdokymenko, V.O. (2023) Sustainable processing of lignocellulosic biomass. IOP Conference Series: Earth and Environmental Science. 1254. 012088. https://doi.org/10.1088/1755-1315/1254/1/012088.

[17]	Korinenko, B.V., Sokol, V.S., Tkachenko, T.V., Kamenskyh, D.S., Haidai, O.O., Sheludko, Y.V., Povazhny, V.A., Ruban, S.V. and Yevdokymenko, V.O. (2024) Carbon materials derived from industrial hemp hurd. 12th International conference "Nanotechnology and nano-materials" (NANO-2024) August 21-24, 2024, Uzhhorod, Ukraine. 260.

[18]	Сокол, В.С., Коріненко, Б.В., Гайдай, О.О., Хімач, Н.Ю., Ткаченко, Т.В., Каменських, Д.С., Поважний, В.А., Євдокименко, В.О. (2024) Термоліз костри технічних конопель для одержання ліквідних продуктів. Біоактивні сполуки, нові речовини і матеріали / доп. учасн. ХХХIХ наукової конференції з біоорганічної хімії та нафтохімії (30 травня 2024 р., м. Київ). за загальною ред. А.І. Вовка. Київ: Інтерсервіс, 2024. 251–255. https://drive.google.com/file/d/1oB9uBhRoMnED1lq-wAuG7j2y0Xgk3V7E/edit.

[19]	Kucherenko, V.О., Yevdokymenko, V.О., Tamarkina, Ju.V., Tkachenko, T.V., Kamenskyh, D.S., Redko, А.V., Povazhnyi, V.А. (2024) Nanoporous carbon formation under alkali thermochemolysis of high-ash lignin. 12th International conference "Nanotechnology and nano-materials" (NANO-2024) August 21-24, 2024, Uzhhorod, Ukraine. P. 29

[20]	Barybina, L.O., Tkachenko, T.V., Haidai, O.O., Korinenko, B.V., Kamenskyh, D.S., Sheludko, Y.V., Povazhny, V.A., Bohatyrenko, V.A., Ruban, S.V., Yevdokymenko, V.O. (2024) Structural and morphological features of microcrystalline сellulose from industrial hemp hurd. Chemistry, Physics and Technology of Surface. 15 (4). 524-533. https://doi.org/10.15407/hftp15.04.524.

[21]	Tkachenko, T.V., Haidai, O.O., Kamenskyh, D.S., Sheludko, Y.V., Pavliuk, O.V., Yevdokymenko, V.O. (2024). Physicochemical characteristics of microcrystalline cellulose from switchgrass (Panicum virgatum L.) obtained in the presence of a solid catalyst. Chemistry, Physics and Technology of Surface. 15(1). 57-66. https://doi.org/10.15407/hftp15.01.057

[22]	Tkachenko, T.V., Kamenskyh, D.S., Sheludko, Y.V., Yevdokymenko, V.O. (2022). Structural and morphological features of microcrystalline cellulose from soybean straw. Chemistry, Physics and Technology of Surface. 13(4) 455-466. https://doi.org/10.15407/hftp13.04.455

[23]	Tkachenko, T., Sheludko, Ye., Yevdokymenko, V., Kamenskyh, D., Khimach, N., Povazhny, V., Filonenko, M., Aksylenko, M., Kashkovsky, V. (2022). Physico-chemical properties of microcrystalline cellulose from flax. Appl Nanosci. 12 (4). 1007-1020. https://doi.org/10.1007/s13204-021-01819-2.

[24]	Aksylenko, M.D., Sheludko, Y.V., Tkachenko, T.V., Haidai, O.O., Yevdokymenko, V.O. (2024). Prospects for using composite preparations based on silica nanosols. IOP Conf. Ser.: Earth Environ. Sci. 1415. 012020. https://doi.org/10.1088/1755-1315/1415/1/012020

[25]	Ткаченко, Т.В., Євдокименко, В.О., Каменських, Д.С., Шелудько, Є.В., Аксиленко, М.Д., Кашковський, В.І. (2020), Рослинні відходи як перспективна сировина для одержання базових продуктів органічного синтезу. 6-Й Міжнародний Конгрес Сталий Розвиток: Захист Навколишнього Середовища. Енергоощадність. Збалансоване Природокористування 23-25 вересня 2020 р., 2020, Львів. С. 171. https://science.lpnu.ua/sites/default/files/attachments/2018/aug/14051/abstracts2020.pdf

[26]	Павлюк, О.В., Ткаченко, Т.В., Євдокименко, В.О., Каменських, Д.С., Кашковський, В.І. (2021). Каталітична конверсія целюлози та лігніну в напрямку отримання рідких високооктанових добавок. 6-Й Міжнародний Молодіжний Конгрес Сталий Розвиток: Захист Навколишнього Середовища. Енергоощадність. Збалансоване Природокористування. 9-10 лютого 2021 р., 2021, Львів. 165. https://science.lpnu.ua/sites/default/files/attachments/2021/jan/23053/youthcongressproceedings2021_0.pdf

[27]	Павлюк, О.В., Ткаченко, Т.В., Кашковський, В.І. (2018) Одержання оксиальдегідів з рослинної сировини. Тези доповідей І Міжнародної (ХІ Української) наукової конференції студентів, аспірантів і молодих учених «Хімічні проблеми сьогодення» (ХПС-2018). Вінниця 27–29 березня 2018 року. 169. https://drive.google.com/file/d/1eoYTvDom6Ty1WzlSDFaG-FHwu0V2YXsh/view