Concentration %  (C) and the degree of urea release (SUM)  – sample no. 1.22.

75% release, 90 days

Time, days

Concentrations, %

90

75

SUM, %

C, %

Granulated slow-release fertilizers based on urea and flue gas desulfurization gypsum

S. Schab1,  M. Borowik2
1. Łukasiewicz Research Network – New Chemical Syntheses Institute, Fertilizer Research Group,

Al. Tysiąclecia Państwa Polskiego 13a, 24-110 Puławy, Poland,

E-mail: sebastian.schab@ins.lukasiewicz.gov.pl

This paper presents the results of a research on a process for production of a calcium sulphate and urea adduct and a method to slow down the release of nitrogen by coating the fertilizer granules with polymers.

Кеуwords: urea, FGD gypsum, granulation, slow realease fertilizers

- Introduction

In the years 2010-2012, at the Łukasiewicz Institute of New Chemical Syntheses, as part of a development project, the technology of granulated nitrogen-calcium-sulfur fertilizer based on phosphogypsum and urea containing an adduct of calcium sulphate and urea (CaSO4⸱4CO(NH2) was developed [1]. Agricultural plot research at the Institute of Soil Science and Plant Cultivation State Research Institute showed that fertilizers produced according to the developed technology, that were used before sowing, have been characterized by a slight slowdown in the nitrogen release. The pre-sowing used in one dose in rapeseed and wheat cultivation showed no worse yielding effects than ammonium nitrate used in two doses. However, the granules of this fertilizer were characterized by an unfavourable shape, significant porosity and a rough surface (Fig. 1). The encouraging results of agricultural research prompted us to work on developing the adduct granulation technique and improving the slowing down of nitrogen release [2-5].

Fig.1. Photograph of the adduct obtained in the semi-technical plant test in 2011

- Methodology and tests results

The aim of the work was to increase the quality of the adduct granules and to develop an economical method of producing fertilizer with a slow release of nitrogen by coating the fertilizer granules with polymers.

Semi-technical tests of NCaS fertilizer production and granulation were carried out in the pilot unit of Łukasiewicz-INS (Fig. 2).

Fig.2. Diagram of a semi-pilot plant for the production of granulated fertilizers at Research Centre at Łukasiewicz-INS

The basic raw materials used were urea fertilizer (produced by G.A. Z.A. Puławy SA) and synthetic calcium sulphate hemihydrate from the flue gas desulfurization process with a grain size of less than 100 µm, (produced by Dolina Nidy Sp. z o.o.). A urea solution with a concentration of 80-90% by mass was sprayed onto the material in a granulation plate to which recycle and gypsum were continuously dosed at a temperature of approximately 55-65°C. Granules were produced in the granulation pan, fed into a drum dryer and, after classification on sieves, a granulated product (adduct) was obtained. Thanks to the use of the synthetic semi-aqueous gypsum (FGDG) and ground adduct recycling, the adduct granules were obtained with a spherical shape and a fairly smooth surface, which turned out to be useful for applying polymer coatings (Fig. 3).

Fig. 3. NCaS fertilizer granules obtained during a semi-technical tests

The adduct granules were coated with coating agent using a laboratory coating unit (Fig. 4). The coating agent was applied to the granules in a rotating bed of material (Fig. 4) in 3 layers at a temperature of 80-90°C, maintained by irradiation with an infrared radiator. According to the new EU fertilizer Regulation 2019/1009, the fertilizer polymer coating should decompose by 90% in soil conditions within 4 years [6].

Fig. 4. Laboratory unit for coating fertilizers with a Teflon covered drum and an infrared radiator (150W)

The release rate of urea nitrogen from samples of fertilizer granulates was determined in the static tests by measuring the concentration of urea, by measuring the refractive index, in the solution that was in contact with the fertilizer sample at specific time intervals under conditions according to the methodology used in Japanese laboratories [7], (10 g of fertilizer / 200 g of water, differing slightly from those described in the EN 13266:2003 standard [8] where 10 g of fertilizer / 500 ml of water is used).

75% release, 90 days

Time, days

90

75

SUM, %

The NCaS granules were coated three times with coating agent (Fig.5.) in a total amount of 4% by mass. The time of applying and hardening of 3 layers of the coating did not exceed 50 minutes. The release time of 75% of nitrogen from this sample in the static test was approximately 90 days (Fig. 6).

Fig.5. Photo - view of coated NCaS fertilizer granules

Fig.6. Concentration (C, %) and urea release rate (SUM) from sample no. 1/22. (nitrogen release tests started immediately after the coating was made)

The degree of urea release SUM (in %) was determined as the ratio of the percentage concentration of urea of the tested sample solution (C) to the concentration of the solution obtained against the parallel ground reference sample (Cz).

SUM=CCz×100%					(1)

- Conclusions

- An economical method of production of granulated nitrogen-calcium-sulfur (NCaS) fertilizer with slow nitrogen release, containing 27% N, 11% Ca, 8.5% S, was developed.

- The NCaS fertilizer contains 4% (by weight) of epoxy resin. The production process is feasible. Further works – scalling up of the coating proces.

- The production process is feasible. Further works will focus on scalling up the coating process.

- The nitrogen release time is over 3 months, it can be adjusted according to the quantity/thickness of the coating.

- Agricultural pot tests on the rapeseed, showed excellent effectiveness of the developed fertilizer, more than doubling the yield of rapeseed seeds compare to control objects.

- References

[1]	Borowik M., Malinowski P., Biskupski A., Dawidowicz M.. Schab S., Rusek P., Igras J., Kęsik K. (2012). Production technology of nitrogen-sulphur-calcium fertilizers on the base of urea and phosphogypsum. Chemik, 66, 5, 525- 434, https://yadda.icm.edu.pl/baztech/element/bwmeta1.element.baztech-article-BPP3-0001-0023/c/Borowik_eng.pdf

[2]	Lawrencia, D.; Wong, S.K.; Low, D.Y.S.; Goh, B.H.; Goh, J.K.; Ruktanonchai, U.R.; Soottitantawat, A.; Lee, L.H.; Tang, S.Y. Controlled Release Fertilizers: A Review on Coating Materials and Mechanism of Release. Plants 2021, 10, 238. https://doi.org/10.3390/plants10020238

[3]	Wesołowska, M., Rymarczyk, J., Góra, R., Baranowski, P., Sławiński, C., Klimczyk, M., ... & Schimmelpfennig, L. (2021). New slow-release fertilizers-economic, legal and practical aspects: a Review. International Agrophysics, 35(1), 11-24. doi: 10.31545/intagr/131184

[4]	Dutta, S., Karak, N., Saikia, J.P. et al. Biodegradation of Epoxy and MF Modified Polyurethane Films Derived from a Sustainable Resource. J Polym Environ 18, 167–176 (2010). https://doi.org/10.1007/s10924-010-0161-8

[5]	Eliaz, N.; Ron, E.Z.; Gozin, M.; Younger, S.; Biran, D.; Tal, N. Microbial Degradation of Epoxy. Materials 2018, 11, 2123. https://doi.org/10.3390/ma11112123

[6]	Regulation (EU) 2019/1009 of the European Parliament and of the Council

[7]	Trenkel M.E. (2010). Slow- and Controlled-Release and Stabilized Fertilizers: An Option for Enhancing Nutrient Use Efficiency in Agriculture, International Fertilizer Industry Association (IFA) Paris, France, ISBN 978-2-9523139-7-1

[8]

EN 13266:2001, Slow-release fertilizers - Determination of the release of the nutrients - Method for coated fertilizers, Comite Europeen de Normalisation, 2001